## Slide 1: OQA module
Thierry Grosjean
DR, CNRS
Institut FEMTO-ST
03 81 66 64 17
thierry.grosjean@univ-fcomte.fr
Classical description of a quantum emitter

## Slide 3
Quantum technologies
OPTICS
/ Photons
Manipulation of single photons
Where do they come from ???
Single photon generator ???

## Slide 4
A model of a fluorescent emitter:
2 energy levels (2 states: fundamental / excited)
Single photon emission: fluorescence
hn1
hn2
n1 > n2
1 photon
absorbé
1 emitted photon

## Slide 5
Fluorescence molecules
Colloidal quantum dots
NV color centers in diamond

## Slide 6
Quantum emitters
- Point-like emitters of light (nanometer scale) : atoms, molecules , nanoparticules.
Internal energy levels  light matter interaction: ground and excited states: emission shows discrete spectral peaks
Spontaneous emission of photons (no stimulated emission)

## Slide 7
Quantum emitters
- Point-like emitters of light (nanometer scale) : atoms, molecules , nanoparticules.
Internal energy levels  light matter interaction: ground and excited states: emission shows discrete spectral peaks
Spontaneous emission of photons (no stimulated emission)
From a classical point of view ??
The dipole

## Slide 8
Radiation of a dipole
Numerical simulation
FDTD method
Fullwave (Synopys)
Dipole

## Slide 9
FDTD method: Finite Difference Time Domain
- Maxwell’s equations resolved in space and time.
- Developed for the first time by Yee in 1966 for the low frequencies (microwaves, etc.)
- The acronym FDTD has been given by Taflove in his reference book, extension to optics
- Widely used in optics for the design and simulations of nano-optical structures.

## Slide 10
Discretization of the Maxwell’s equations in space and time
Space gridding
View of the field components in a single cell : the Yee cell

## Slide 11
- Boundary conditions with neighbouring cells
How does it work ? The algorithm
- The space and meshgrid (in space and time)  computation volume
t
- We place the EM source: source term =
- generates et dans in the cell (Maxwell’s equations)
- Field propagation in the cell (finite diff.)
- Stationnary regime reached: we stop
- We define objects: e defined in each cell

## Slide 12
Comments
1- Finite computation volume
 the optical waves are reflected at the edges !!!!!!
Absorbing layer:
PML (Perfectly Matched layer)
2- Spatial and temporal discretizations are linked
 A rule must be fulfilled !!  stability criterion

## Slide 13
FDTD, commercial software « Fullwave »

## Slide 14
MISSION #1
Characterize the EM field around the dipole
E-field
H-field
Dipole: classical analog of a quantum emitter (that is, a point-like source)
 Take the user’s guide

## Slide 15
x
y
z
E-field
Ex
Ez

## Slide 16
x
y
z
H-field

## Slide 17
E
H
Axial symmetry

## Slide 18
MISSION #2
Calculate the power radiated by a dipole
1- Dipole in vacuum
2- Dipole near an object

## Slide 19
 Poynting theorem (cf. Novotny’s book)
E and H fields (FDTD)
Power

## Slide 20
Poynting theorem
Net energy flow through the surface S delimiting a volume V
Rate of change of the energy inside the volume
Rate of energy dissipation within the volume (by the Lorentz force (F=E) acting on charges densities )
In a linear and non dispersive medium
The exerted work
Poynting

## Slide 21
Poynting theorem
Net energy flow through the surface S delimiting a volume V
Rate of change of the energy inside the volume
In a linear and non dispersive medium
Poynting
RADIATION AND ABSORPTION (joule effect)

## Slide 22
Poynting theorem
Harmonic fields in time (stationary regime), linear and non dispersive fields
Time-averaged quantities

Time averaged Poynting vector
 =
In complex notation

## Slide 23
S
V
j2
Absorption
Joule effect, etc.
V2
j1
Source
 radiation
V1
An example

## Slide 24
S
V
j2
Absorption
Joule effect, etc.
V2
j1
Source
 radiation
V1
An example
Power outside V
= Power radiated inside V – Power absorbed inside V

## Slide 25
S
V
j2
Absorption
Joule effect, etc.
V2
Power outside V
= Power radiated inside V – Power absorbed inside V
j1
Dipole
Point-like source
The source = dipole

## Slide 26
x
y
z
M
0
Radiating dipole
(in Harmonic regime)
Current density
In first approximation, we have:
Dipole moment
Due to a charge distribution q of coordinate

## Slide 27
From the Poynting theorem
Dissipated energy by time unit = radiated power
Volume of the source
For a dipole, is replaced by :
Radiated electric optical field at the dipole position

## Slide 28
Dipole in an inhomogeneous medium
The back-scattered field changes the power
Cf. Principle of nano-optics, L. Novotny, Cambridge, 2e Ed. 2012, p239

## Slide 29
An oscillating charge produces
an electromagnetic radiation
Mediates the energy dissipation from the dipole source
Has an influence back onto the oscillating charge (!!)
Retroaction of the radiating dipole on itself due to the environment

## Slide 30
MISSION #2
Calculate the power radiated by a dipole
1- Dipole in vacuum
2- Dipole near an object

## Slide 31
S
V
j2
Absorption
Joule effect, etc.
V2
Power outside V
= Power radiated inside V
j1
Dipole
Point-like source
The source = dipole
– Power absorbed inside V
vacuum
?

## Slide 32
Calculation of the Poynting vector flow !
Poynting’s theorem
S
dipole
e
Time averaged
Power outside V = Power radiated inside V

## Slide 33
MISSION #2
Calculate the power radiated by a dipole
1- Dipole in vacuum
2- Dipole near an object

## Slide 34
S
V
j2
Absorption
V2
j1
Dipole
Power radiated by the system « dipole+object »
Poynting vector flow ?

## Slide 35
S
V
j2
Absorption
V2
j1
Dipole
Power radiated by the dipole
Poynting vector flow ?
BUT… numerical artifacts when the distance DIPOLE-OBJECT is small… OUR CASE

## Slide 36
No Choice !!!!
j2
Absorption
Joule effect, etc.
V2
j1
Dipole
?
FDTD

## Slide 37
Dipole in a homogeneous medium
Calculation of
Whose permittivity e matches that of the medium at the dipole position, when the dipole interacts with the nanostructures
e
STEP #1 :
STEP #2 :

## Slide 38
x
y
z
0
Cf. Principle of nano-optics, L. Novotny, Cambridge, 2e Ed. 2012, p239
In a homogeneous medium  analytical expression of E
STEP #1 :

## Slide 39
dipole
S
e
From analytical expression of the E-field
From FDTD calculation
STEP #1 :

## Slide 40
- Normally =0  and are in phase
- With the FDTD (not null…)
STEP #2 :
In a homogeneous medium
In a inhomogeneous medium, remains unchanged

## Slide 41
, )
STEP #2 :
 Dipole in vacuum (a homogeneous medium)
Dipole along (0x)
There are two solutions, only one is correct, to be tested by recalculating P

## Slide 42
Dipole interacting with nanostructures
FDTD
known

## Slide 43: OQA module
Thierry Grosjean
DR, CNRS
Institut FEMTO-ST
03 81 66 64 17
thierry.grosjean@univ-fcomte.fr
Classical description of a quantum emitter

## Slide 44
Introduction
  Definition of a quantum emitter (QE)
  3 types of emitters
Individual QE in an inhomogeneous environment
Description via the quantum ElectroDynamics (ED) (just basic considerations…)
  Description of the spontaneous emission
  Description of the excitation
  Description of fluorescence emission
Description of the spontaneous emission by the classical ED
  Classical electrodynamics ?
  Link between quantum and classical ED

## Slide 45: I- Introduction

## Slide 46
Quantum emitter:
- Light emitter (in our case)
Point-like emitter (nanometer scale) : atoms, molecules , nanoparticules.
Internal energy levels  light matter interaction: ground and excited states: emission shows discrete spectral peaks
« states »  electrons in orbitals defined by quantum numbers (n,l, ml, ms)
Single photon emissions
Spontaneous emission of photons (no stimulated emission)
central in nano-optics or nano-photonics

## Slide 47
The model of a fluorescent emitter:
2 energy states (fundamental / excited states)
Single photon emission: fluorescence
hn1
hn2
n1 > n2
1 photon
absorbé
1 emitted photon

## Slide 48
3 families of quantum emitters:
Fluorescent molecules
Quantum dots
Color centers (in diamond)

## Slide 49
Fluorescence molecules
 Organic molecules
 Elongated shape !!
Jablonski Diagram
 Energy states

## Slide 50
Point-like fluorescent sources Dipole sources
Transition dipole moment
 For absorption and emission
Taux de fluorescence R
d
From the spatial point of view…
 Oriented Dipole moment

## Slide 51
3 families of quantum emitters:
Fluorescent molecules
Quantum dots
Color centers (in diamond)

## Slide 52
Colloidal quantum dots
 Semiconductor nanocristals in solution
 Almost spherical shape
 Size: on the nanoscale
Quantum dots CdSe/Zns of various sizes (1 size per bottle) – UV excitation

## Slide 53
*0,00000014
*0,00000014

## Slide 54
 Properties of Semiconductors + « quantum size effect »
 QD = « big atom »: two energy state system with a particle of 2-6 nm, i.e., 10 to 100 bigger than an atom  easier manipulation, etc…

## Slide 55
électron
illumination
Conduction
band
Valence
band
electron
hole
recombinaison
excitation
Single photon
Fluorescence: involves an exciton rather than an electron
Exciton = electron-hole pair (semiconductor material)

## Slide 56
électron
illumination
Bande de conduction
Bande de valence
électron
trou
recombinaison
excitation
Single photon
Fluorescence: involves an exciton rather than an electron
Exciton = electron-hole pair (semiconductor material)

## Slide 57
High emission yield/efficiency at room temperature
Photostability at room temperature
QD encapsulation: « core-shell » system
Avantages:
- Broadband absorption (semiconductor)
- quantum size effect: the size defines the emission wavelength
- Photon sources from blue to near and middle infrared !!
- Photostability at room temperature  no expensive cooling
Drawbacks :
blinking
In contact to O2, blueshift of the emission wavelength

## Slide 58
Broad application field: biomedical (fluorescent markers), optoelectronics, screens-TV, etc…
Dipole :
 Dipolar transitions for the absorption et emission (as molecules) excepted that:
Degenerated dipole moment:
Dipolar emission in a 2D plan,
Arbitrary orientation of the mission dipole in this plane (no fixed oriented dipole)
Quantum dot imaging
Molecule imaging

## Slide 59
3 families of quantum emitters:
Fluorescent molecules
Quantum dots
Color centers (in diamond)

## Slide 60
Vacancy in a high energy gap (5.5 eV) semiconductor: diamond
A single nitrogen atom (N) creates on a neighbouring site a vacancy  « NV center »
Free electron are in play  favorable to fluoresence
Lifetime of the excited state: 11 ns
Size: 10-30 nm (size of the diamond fragment which hosts the NV-center)
Easier manipulation than QDs  attached at the very tip
No blinking
Fixed emission wavelength = 690 nm (no wavelength tunability)
Also used as a probe for magnetometry

## Slide 61
The fluorescence, this is…
These two steps are rigorously described using quantum electrodynamics
Tiny objects on the nanoscale  quantum theory
A two-step process:
Absorption of a photon
Spontaneous emission of a photon of (usually) lower energy  Stokes shift

## Slide 62
Introduction
  Definition of a quantum emitter (QE)
  3 types of emitters
Individual QE in an inhomogeneous environment
Description via the quantum ElectroDynamics (ED) (just basic considerations…)
  Description of the spontaneous emission
  Description of the excitation
  Description of fluorescence emission
Description of the spontaneous emission by the classical ED
  Classical electrodynamics ?
  Link between quantum and classical ED

## Slide 63
Purcell (1946) : spontaneous emission of a QE is modified by its environment
 QE coupled to an optical resonator (resonant optical structure such as a FP cavity, etc.)
Purcell Factor:
Purcell effect: if high Q and small V, a QE emits its photon much faster : « super emitter »
Volume of the resonant optical mode
Quality factor of the resonator
Enhancement of the emission rate

## Slide 64
Fluorescence lifetime modified by a non resonant optical environement
n
1
Drexhage et al, 1966
 Purcell effect experimentally demonstrated (Goy et al, 1983)
 Inhibition of the spontaneous emission in a resonant cavity (that is the opposite effect to Purcell’s… in a cavity !!) (Kleppner, 1981)
Since Purcell (1946)
1966
1981-1983
Since 2000,
Engineering of the spontaneous emission

## Slide 65
By structuring the environment of a QE…
Nanotechnologies
New fabrications facilities on the nanoscale
 Full control over light-matter interaction
nano-optics
We modify its photon absorption/emission properties
We control its photon absorption/emissionproperties
20th centery
21th centery

## Slide 68
Need of on-demand single photon sources of controlled properties and performances
Quantum emitters  Single photon sources
The starting point of future quantum technologies
WHY ?
 nano-photonics could fullfil this requirement by accurately structuring the environment of the QE

## Slide 69
Introduction
  Definition of a quantum emitter (QE)
  3 types of emitters
Individual QE in an inhomogeneous environment
Description via the quantum ElectroDynamics (ED) (just basic considerations…)
  Description of the spontaneous emission
  Description of the excitation
  Description of fluorescence emission
Description of the spontaneous emission by the classical ED
  Classical electrodynamics ?
  Link between quantum and classical ED

## Slide 70
QE in an inhomogeneous environment
object
QE
hn1
excitation
|e>
|i>
2-state model
decay
3 decay channels
hn2

## Slide 71
: excitation rate
: radiative decay rate  Fluo
: non-radiative decay rate
due to losses in the environement
 only can be experimentally measured
: intrinsic non-radiative decay rate
excitation
|e>
|i>
relaxation

## Slide 72
Description of the spontaneous emission
excitation
|e>
|i>
decay

## Slide 73
Total decay rate
Non-radiative decay rate
Particular case, QE in vacuum
 Intrinsic losses which are independent of the QE env.
vacuum
 Spontaneous emission influenced by the environment of the QE (Purcell and others)

## Slide 74
Lifetime of the excited state
Emitter in vacuum

## Slide 75
Quantum yield (efficiency)
Probability of a radiatively released photon
Probability of a radiative decay
Emitter in vaccum
Intrinsic quantum yield

## Slide 76
Description of the QE excitation
excitation
|e>
|i>
decay

## Slide 77
Case of an QE excitation with weak optical power : excitation well below the saturation regime
Iexc
Signal fluo
saturation
Emitter in vacuum
unit vector defining the dipole moment of the QE
: electric optical field for excitation
: position vector of the QE
: angular frequency at excitation
 The QE is most of the time in its ground state

## Slide 78
Description of fluorescence emission
excitation
|e>
|i>
relaxation

## Slide 79
below saturation threshold
Fluorescence rate
Experimentally measurable parameter (with a photon counter)

## Slide 80
Introduction
  Definition of a quantum emitter (QE)
  3 types of emitters
Individual QE in an inhomogeneous environment
Description via the quantum ElectroDynamics (ED) (just basic considerations…)
  Description of the spontaneous emission
  Description of the excitation
  Description of fluorescence emission
Description of the spontaneous emission by the classical ED
  Classical electrodynamics ?
  Link between quantum and classical ED

## Slide 81
excitation
|e>
|i>
decay

## Slide 82
Why ?
Nanoscale systems : « QE + environment » are often too complex to be rigorously resolved/described by quantum electrodynamics
Classical Electrodynamics is much more simple to implement
 Numerous numerical methods based on Maxwell’s equations are nowadays commercially available (FDTD, FMM, etc.)

## Slide 83
Électrodynamique classique ?
QE  Radiating dipole
object
dipole
Power calculation from electromagnetic waves
Electromagnetic waves
 Poynting’s theorem

## Slide 84
Quantum formalism of the QE
Classical formalism of the radiating dipole
The link between
quantum and classical electrodynamics
In the case of a « weak coupling » between the QE and its environment, we have:
IMPORTANT !

## Slide 85
A link between quantum and classical approaches is possible at the expense of a normalisation process
We can only predict a relative spontaneous emission induced by the environment of the QE. No quantitative prediction of the emission rate…
BUT the problem is greatly simplified

## Slide 86
In the following: PERFECT EMITTERS
excitation
|e>
|i>

## Slide 87
hn
2 decay channels to simulate
1
2
excitation
|e>
|i>
Problem to resolve

## Slide 88
What do we have ?
Numerical methods based on Maxwell’s equations
Analytical description of a radiating dipole
 dipolar field (analytic formula)
Poynting’s theorem
Classical electrodynamics

## Slide 89
TP :
Spontaneous emission (SE) of a quantum emitter near a structure : quantum description via classical electrodynamics

## Slide 90
Objective
Prediction of the change of SE of a single emitter positioned near a (nano)structure
2 cases under study :
// (0x)
// (0z)
Au
Air
x
y
z
Emission at l = 800 nm

## Slide 91
Methodology
Quantum formalism of the QE
Classical formalism of the radiating dipole
 Power calculation from a radiating dipole
P0 and P have to be calculated with the dipole positioned in two media of the same permittivity !!!
e

## Slide 92
Methodology
Quantum formalism of the QE
Classical formalism of the radiating dipole
S
e
S
e
e

## Slide 93
Methodology
=